SECTION 12 48 13

ENTRANCE FLOOR MATS AND FRAMES

**eleGRIL® Stainless Steel Grates**

PART 1 – GENERAL

1. SUMMARY
   1. Section Includes
      1. Entrance floor mats, grids, and frame assemblies.
   2. Related Requirements
      1. Division 03 - Cast-In-Place Concrete: For concrete floor slab recess, and grouting frames into recess.
      2. Division 07 - Damp-proofing.
      3. Division 23 - Sanitary Waste and Vent Piping: For floor drain if applicable.
2. REFERENCES

A. ASTM B 221-93 Standard Specification for Aluminum and Aluminum-Alloy Extruded Bars, Rods, Wire, Shapes, and Tubes

B. ASTM A 276-92 Standard Specification for Stainless and Heat-Resisting Steel Bars and Shapes.

C. AAMA 606.1 Voluntary Guide Specifications and Inspection Methods for Integral Color Anodic Finishes for Architectural Aluminum

D. AAMA 607.1 Voluntary Guide Specifications and Inspection Methods for Clear Anodic Finishes for Architectural Aluminum.

1. COORDINATION
   1. If product is to be recessed, coordinate with concrete work so that products are available for placing integrally with floor slabs.
2. SUBMITTALS
   1. Product Data: Manufacturers product specifications, installation and maintenance instructions.
   2. Shop Drawings: Show layout and types of grates and frames not less than half-scale sections of typical installations, details of patterns or designs, anchors, and accessories, and field measurements of slab recess to receive frames grates (if applicable).
   3. Samples for Selection Purposes: Actual sections of grate and frame material in a convenient but representative size showing full range of colors, textures, finishes and patterns available for each type of floor grate and frame specified.
   4. Samples for Verification Purposes: Not less than 6 inch square sections of grate material and 6 inch length of frame material in selected colors and finishes for each type of grate and frame specified.
   5. Installation, Operations and Maintenance data.
   6. LEED Submittals:

1. Product Data for Credit IEQ 5: Indoor Chemical and Pollutant Source Control: Employ permanent entryway systems at least 10 feet long in the primary direction of travel to capture dirt and particulates entering the building at regularly used exterior entrance.

1. WARRANTY
   1. Provide manufacturer's written warranty.
   2. Warrant materials and fabrication against defects after completion and final acceptance of Work.
   3. Repair defects, or replace with new materials, faulty materials or fabrication developed during the warranty period at no expense to Owner.

PART 2 - PRODUCTS

1. ACCEPTABLE MANUFACTURERS

Nystrom

9300 73rd Avenue North

Minneapolis, MN 55428

PH: 800.547.2635

FX: 800.317.8770

1. DESIGN CRITERIA
   1. Rolling Load: 1000 lbs/wheel.
   2. Uniform Load: 1000 lbs/sq. ft.
2. ENTRANCE SYSTEM FLOOR GRATE **(SPECIFIER TO SELECT ONE BELOW AND DELETE OTHERS)**
3. Model and Description: EleGRIL**®** Stainless Steel Gratings. Type 304 stainless steel per ASTM A 276 available in 7/16”, 5/8”, or 1 1/8” depth. **(SPECIFIER TO SELECT ONE DEPTH AND DELETE OTHERS)**
4. Construction: Surface Wires: .093" (2.4mm) by 0.156" (4mm) wire with 0.070" (1.8mm) support bars spaced 1" (24mm) o.c. Wire spacing shall be 0.233" (5.9mm) o.c.
5. Lockdowns: Hidden
6. Tread wires shall be resistance welded at each joint.
7. Fasteners: Non-corrosive screws and anchors for securing frames together and to floors.
8. Rail finish shall be mill.
9. Unit must meet rolling load of 1000 lb/wheel. Uniform load of 1000 lbs/sq.ft.
10. Model and Description: EleGRIL**®** Stainless Steel Gratings with UltraSorb Carpet Inserts. Type 304 stainless steel per ASTM A 276 available in 7/16” depth. **(SPECIFIER TO SELECT ONE DEPTH AND DELETE OTHER)**
    1. Construction: Surface Wires:.093" (2.4mm) by 0.156" (4mm) wire with 0.070" (1.8mm) support bars spaced 1" (24mm) o.c. Wire spacing shall be 0.233" (5.9mm) o.c.
    2. Lockdowns: Hidden
    3. Tread wires shall be resistance welded at each joint.
    4. Fasteners: Non-corrosive screws and anchors for securing frames together and to floors.
    5. Rail finish shall be mill.
    6. Unit must meet rolling load of 1000 lb/wheel. Uniform load of 1000 lbs/sq.ft.
    7. UltraSorb tread insert: tufted nylon with a polyester non-woven primary backing and stiff secondary backing. Class 1 fire-rated; pile weight 35 oz. per square yard (950 grams per square meter). Available colors include: Stormy Blue, Briar, Flannel, Ink, and Black,
11. Model and Description: EleGRIL stainless steel grate with Rugged Scrub premium absorbent treads. Type 304 stainless steel per ASTM A 276 available in 7/16” depth**. (SPECIFIER TO SELECT ONE AND DELETE OTHER)**
12. Construction: Surface Wires: 093" (2.4mm) by 0.156" (4mm) wire with 0.070" (1.8mm) support bars spaced 1" (24mm) o.c. Wire spacing shall be 0.233" (5.9mm) o.c.
13. Lockdowns: Hidden
14. Tread wires shall be resistance welded at each joint.
15. Fasteners: Non-corrosive screws and anchors for securing frames together and to floors.
16. Rail finish shall be mill.
17. Unit must meet rolling load of 1000 lb/wheel. Uniform load of 1000 lbs/sq.ft.
18. Rugged Scrub tread insert: Crimped solution-dyed 600 denier polypropylene fibers, tufted into a woven double backing and mechanically secured to tread rails. ). Available colors include: Charcoal, Chocolate Chip, Licorice, Tan, Navy, Teal or Red.
19. ENTRANCE SYSTEM GRATE FRAME **(SPECIFIER TO SELECT ONE BELOW AND DELETE OTHERS)**
20. Model F-8: Cast-in Place, Level Bed aluminum frame, Extruded aluminum; 1/8” profile; 1 11/16” overall depth. Frame finish shall be supplied in mill (standard) or one of 10 optional colors as offered by manufacturer. (Call factory for custom colors).
21. Model F-12: Aluminum Surface Mount frame, Extruded 6063-T5 aluminum alloy. 1 5/8” profile; 15/32” overall depth. Frame finish shall be supplied in clear mill. Model F-12
22. Model F-13: Cast-in Place, Level Bed aluminum frame, Extruded aluminum; 1/8” profile; 1 1/16” overall depth. Frame finish shall be supplied in mill (standard) or one of 10 optional colors as offered by manufacturer. (Call factory for custom colors).
23. Model SS-38SF: Level Bed Stainless Steel frame, Type 304 stainless steel; 1/8” profile; 9/16” depth. Finish: Finish: #4 Satin
24. Model 38-SFD: Level Bed Stainless Steel frame, Type 304 stainless steel; 1/8” profile; 9/16” depth. Finish: Finish: #4 Satin, pre-drilled.
25. Model SS-58SF Level Bed Stainless Steel frame, Type 304 stainless steel; 1/8” profile; 3/4” depth. Finish: Finish: #4 Satin
26. Model SS-98SF Deep Pit Stainless Steel frame, Type 304 stainless steel; 1/8” profile; 1 1/4” depth. Finish: Finish: #4 Satin. *Note: Rolling load capacity for this application is 300 lb/wheel*.
27. Model SS-98SFLB Level Bed Stainless Steel frame, Type 304 stainless steel; 1/8” profile; 1 1/4” depth Finish: #4 Satin

PART 3 - EXECUTION

1. EXAMINATION
2. Products must be placed on a flat and level substrate. Substrate shall meet tolerance of 1/8" over 10 feet in accordance with ACI 302.
3. Examine areas and conditions under which Work is to be performed and identify conditions detrimental to proper or timely completion.
   * + 1. Do not proceed until unsatisfactory conditions have been corrected.
4. INSTALLATION
5. Install products in accordance with manufacturer’s instructions, at locations shown and with top of products level with adjoining finished flooring where applicable.
6. Coordinate top of product surfaces with swinging doors to provide under-door clearance.

1. Provide necessary shims, spacers, and anchorages for proper location and secure attachment of frames to concrete.

2. For installation in terrazzo flooring, contact manufacturer.

1. ADJUSTING AND CLEANING

A. Adjust top surface of assembly to be flush with adjacent finishes.

B. Coordinate top of surfaces with doors that swing across surface to provide adequate underdoor clearance.

C. Clean dirt and debris from frame recess before installing floor system.

1. PROTECTION
2. Upon completion of frame installations, provide temporary filler of plywood or fiberboard in grate recesses, and cover frames with plywood protective flooring. Maintain protection until construction traffic has ended and Project is near time of Substantial Completion.
3. Install product when no further wheeled construction traffic will occur and wet type operations including painting and decorating are complete.

END OF SECTION