3-Part CSI MasterFormat Specification

SECTION 08 3123

Floor DOORs AND FRAMES

Rev 11/22

- GENERAL

      - SUMMARY

        - Section includes:

          - Floor Doors for access between building floors as indicated on drawings and specified herein

      - references

        - Aluminum Diamond Tread Plate:  ASTM B632-02, 1/4 inch 6061-T6 aluminum with mill finish.

        - Aluminum Extrusion:  6061-T6 aluminum.

        - Steel Diamond Tread Plate:  ASTM A786.

        - Steel Angle:  ASTM A36-94 steel frame, structural.

        - Stainless Steel Diamond Tread Plate:  ASTM A793 stainless steel, No. 304 finish.

        - Stainless Steel Angle:  ASTM A276 stainless steel, No. 304 finish.

        - Stainless Steel Smooth Plate:  ASTM A240 smooth plate stainless steel, type No. 316.

        - Fasteners:  Type No. 316 stainless steel.  ASTM F593 for bolts and ASTM F594 for nuts.

        - General:  Comply with NAAMM's "Metal Finishes Manual for Architectural and Metal Products" for recommendations for applying and designating finishes.

      - Action SUBMITTALS

        - Shop Drawings: Indicate configuration and dimensions, show components, adjacent construction, required clearances and tolerance and other affected work.

        - Product Data:  Manufacturer’s technical data for each type of floor door, including setting drawings and finish requirements

      - informational submittals

        - Provide manufacturer's standard warranty.

        - Sustainable Design Submittals:

          - Building Product Disclosure Requirements: To encourage the use of building products that are working to minimize their environmental and health impacts, provide the following information when available:

            - Material Ingredients Documentation demonstrating the chemical inventory of the product

      - Closeout submittals

        - Manufacturer's Installation Instructions and Operation & Maintenance:  Indicate installation, operation and maintenance requirements and rough-in dimensions.

      - Quality Assurance

        - Qualifications:

          - Manufacturer/Installer:  Company specializing in manufacturing and installation of components specified in this Section with minimum of 5 years documented experience.

        - Regulatory Requirements:

          - International Building Code for fire resistance rated construction

          - IBC Section 712 for Floor Fire Doors- tested in accordance with NFPA 288 and labeled by approved agency; Warnock Hersey or Underwriters Laboratory.

- PRODUCTS

      - MANUFACTURER

        - Nystrom

9300 73rd Ave N

Minneapolis, MN  55428

PH: 800-547-2635

www.Nystrom.com

      - ALUMINUM FLOOR DOORS

        - Angle Frame Water Tight Aluminum Floor Door: Model FDWTA

          - Clear Unobstructed Opening Size: <Insert dimensions>.

          - Frame: Mill finish aluminum, 1/4 inch (6.4 mm) aluminum, mill-finish.

          - Door: Single leaf; 1/4-inch-thick (6.4-mm-thick), diamond-pattern mill-finish aluminum plate.

Manufacturers' offerings for loading capacity vary; confirm availability. See the Evaluations for discussion of AASHTO H20.

          - Loading Capacity: 650-lbf/sq. ft. (31.1-kN/sq. m) live load with a maximum deflection of L/150 and watertightness to 10 ft (3.05 m) water column.

          - Gasket: EPDM water and odor resistant.

          - Hardware:

            - Material and Finish: Type 316 stainless steel, including latch, handle, lifting mechanism assemblies, hold-open arms, brackets, hinges, pins, and fasteners.

            - Hinges: Heavy-duty butt hinges with stainless-steel pins fastened to door with stainless steel carriage bolts.

            - Operating Mechanism: Adjustable Type 17-7 stainless steel counterbalancing spring enclosed in a telescoping tube, heavy-duty hold-open arm that automatically locks door open at 90 degrees, release handle with red vinyl grip that allows for one-handed closure, and recessed lift handle.

            - Latch: Type 316 Stainless-steel pressure locks.

          - Optional Lock: External Padlock Hasp

          - Safety Accessories: Safety [grate] [chains] [net] [railing] [telescoping safety post] <Insert safety device>

- EXECUTION

      - EXAMINATION

        - Verify that preparation and affected dimensions are acceptable.

        - Verify tolerances and correct improper conditions.

      - PREPARATION

        - Advise installers of details relating to floor hatch installation, including rough opening dimensions, locations of supports, and anchoring methods.

      - INSTALLATION

        - Follow manufacturer’s instructions for installing floor doors and hatches.

        - Install frames plumb and level in opening, in proper alignment with floor surface for flush installation.  Secure rigidly in place.

        - Position units to provide convenient access to concealed Work requiring access.

      - ADJUSTING

        - Operational Units:  Test-operate units with operable components.

        - Clean and lubricate joints and hardware.

        - Adjust for proper operation.

      - CLEANing

        - Clean adjacent surfaces and remove unused product and debris from site.

        - Adjust doors for smooth operation.

END OF SECTION