3-PART CSI MASTERFORMAT SPECIFICATION

SECTION 079513

EXPANSION JOINT COVER ASSEMBLIES

PART 1 - GENERAL

1.01	Work Included

- The work shall consist of furnishing and installing molded elastomeric hinged cover systems in accordance with the details shown on the plans and the requirements of the specifications.  The molded elastomeric hinged cover systems are proprietary designs utilizing extruded rubber covers integral with independent metal plates.

- Related Work

- Cast-in-place concrete

- Miscellaneous and ornamental metals

- Flashing and sheet metal

- Sealants and caulking

1.02	Submittals

- Template Drawings - Submit typical molded elastomeric hinged cover system cross-section(s) indicating pertinent dimensioning, general construction, component connections, and anchorage methods.

1.03	Product Delivery, Storage and Handling

- Deliver products in each manufacturer's original, intact, labeled containers and store under cover in a dry location until installed. Store off the ground, protect from weather and construction activities.

1.04	Acceptable Manufacturer

- Subject to compliance with requirements, provide products from the following:

Nystrom
9300 73rd Avenue North
Minneapolis, MN 55428
PH: 800.547.2635
www.Nystrom.com

- Any proposed alternate systems must be submitted and approved thirty (30) days prior to the bid.  All post bid submittals will not be considered.  This submission shall be in accordance with MATERIALS AND SUBSTITUTIONS.
- Any manufacturer wishing to submit for prior approval must provide the following:

- A working three (3) foot sample of the proposed system with a letter describing how system is considered superior to the specified system.

- Letter from approved independent laboratory stating that the proposed product’s physical properties and design meet the requirements of the project specification.

- A project proposal drawing that illustrates the recommended alternate system installed in the concrete deck that is specific to the project.  Typical catalog cut sections will not be considered.

- Verifiable list of prior installations showing successful experience with the proposed systems.

- Any substitution products not adhering to all specification requirements within, will not be considered.

- Bidders are presumed by the specifier to furnish the materials specified in specification Section 05800 and related sections unless the bidder clearly stipulates in their bid form their intent to use an alternate material.

The bidder must otherwise clearly submit with the bid, which of the specified products the bid is based upon. Upon award of the project, the bidder will be required to utilize the product that was stipulated in their bid.

The specifier reserves the right to require any bidder to submit supplementary or additional information after bids are opened before approving alternatives. A bidder intending to use an alternative system shall not be eligible for award unless the supporting information has been submitted to the specifier at bid opening and approved prior to award.

1.05   Quality Assurance

- Warranty: The molded elastomeric hinged cover system shall be warranted for a period of one (1) year for normal traffic usage under specified movement limitations and design conditions as described by the manufacturer.

The provided one (1) year warranty shall be a materials only warranty. Manufacturer will supply all materials needed to properly repair or replace defective or damaged product within the term of the warranty.

- Manufacturer: Shall have a minimum ten (10) years experience specializing in the manufacturing of molded expansion joint elastomeric hinged cover systems.  Verification of experience will be required.

PART 2 - PRODUCT

2.01	General

- Provide molded elastomeric hinged cover system that is capable of spanning joint opening based upon movement requirements. Provides a safe transition over natural recesses created by all blockout and cavity type expansion joints. Creates a smooth transition between opposing slabs under vertical displacement. Utilizes extruded ethylene propylene diene monomer (EPDM) with independent steel plates for reinforcement. When installed over a flat surface, “EJ-RCP” shall comply with ADA guidelines. Install all components utilizing recommended fasteners for complete installation.

Furnish Nystrom “EJ-RCP” molded elastomeric hinged cover system as indicated on drawings.

2.02	Components and Materials

- EPDM Rubber Cover: When installed the top surface of the cover profile shall be non-slip and provide a suitable transition across the joint opening.  Material shall be EPDM or manufacturer’s alternate material exhibiting a shore A hardness of 60 +/- 5.

| PHYSICAL PROPERTY | ASTM TEST METHOD | REQUIREMENTS |
| --- | --- | --- |
| Tensile Strength | D 412 | 10.4MPa (1500psi) min. |
| Ultimate Elongation | D 412 | 350% min |
| Hardness, |  |  |
| Shore A 7 days @ -10°C (14°F) | D 2240 | 60 +/- 5 |
| Heat Resistance, |  |  |
| 70 hrs. @ 100°C (212°F) |  |  |
| Tensile Strength Change |  | 25% max |
| Ultimate Elongation Change |  | 25% max |
| Hardness Change | D 573 | 10 pts max |
| Oil Resistance, 70 hrs. @ 100°C (212°F) |  |  |
| Volume Change | D 471 | 120% max |
| Ozone Resistance, |  |  |
| 50 pphm for 70 hrs. @ 104°F | D 518 | 100 quality retention rating |
| Compression Set, 22 hrs. @70°C | D 395 | 50% max |

- Metal plates – Provide 3/16 inch steel plates and 1/4 inch thick (EJ-RCP-600N & EJ-RCP-1000N), 1/2 inch thick (EJ-RCP-1200N & EJ-RCP-1800N), ¾ inch thick (EJ-RCP-3150N) structural steel plates, to accommodate various structural joint sizes and movement requirements. Meets or exceeds HS-20 loading requirements

- Anchors - Provide 3/8 inch dia. by 3 inch long manufacturer’s recommended Heavy Duty Concrete Anchor at 14, 16, or 18 inches o.c. max. spacing. Install anchors in strict accordance with manufacturer’s instructions in sound concrete with 2-1/2 inch minimum anchor embedment.

- Flexible Gutter System (if required) – supply Flexible Gutter System to drain excess amounts of collected moisture. System will satisfy the required design movement and compress without damage.

2.03		Fabrication

- Nystrom “EJ-RCP” shall be shipped in 6 foot lengths (EJ-RCP-600N and EJ-RCP-1000N), 5 foot lengths (EJ-RCP-1200N & EJ-RCP-1800N) and 4 foot lengths (EJ-RCP-3150N on manufacturer’s standard shipping pallet.

- Anchors shall be shipped in manufacturer’s standard carton.

  - Finishes

(Standard)

- Exposed elastomeric surfaces shall be supplied in standard color Pavement Black unless otherwise specified.

(Optional)

- Exposed elastomeric surfaces - available colors:   Concrete Grey or Yellow

PART 3 - EXECUTION

3.01	Installation

- Protect elastomeric hinged cover system from damage during installation of adjacent materials and thereafter until completion of structure.

- Elastomeric hinged cover systems shall be installed in strict accordance with the manufacturer's typical details and instructions along with the advice of their qualified representative.

3.02	Clean and Protect

- Protect system and its components during construction. After work is complete in adjacent areas clean exposed surfaces with a suitable cleaner that will not harm or attack the elastomeric material.

END OF SECTION

REV 02/26